Huaibei SanHe Developing Co., Ltd.

Certificate Of Analysis

Product Name: Cerium Ammonium Nitrate
Date        :2007/07/31

Quantity     :500g

Lot No.:2007072202

Item                                                      =====================================================================
Appearance               :Orange red crystalline powder 

Re:Impurities content          

TREO                   :30.00% Min.             

La2O3                   :90PPM

Y2O3                      :60PPM

Pr6O11                    :70PPM

Nd2O3                     :90PPM

SM2O3                     :70PPM

CeO2/TREO                 :99.95%Min.

Re:Non-Re:Impurities content (Max)

Fe2O3                     :2.5PPM

SO4                       :22PPM

Cl                        :25ppm

CuO                       :0.5PPM

CaO                       :3.0PPM

NiO                       :0.5PPM

Na2O                      :0.5PPM

PbO                       :0.5PPM

===================================================================================
Testing:ZHANG PING                                      DATE:2007/07/31

