Huaibei SanHe Developing Co., Ltd.

Certificate Of Analysis

Product Name: Cerium OXIDE
Date        :2007/07/29

Quantity     :500g

Lot No.:20070729

Item                                                      =====================================================================
Appearance               :PINK POWDER

Re:Impurities content          

TREO                   :99.0% Min.                              99.28%

CeO2/TREO                 :99.8%Min.                               99.95%

Fe2O3                     :0.05%MAX                                0.01%

===================================================================================
Testing:ZHANG PING                                      DATE:2007/07/29

